CSI Format Specification for Ferric™ railings – with Infill and LED options

Part 1 - General:

  - Section Includes

Pre-engineered Ferric™ powder coated steel and stainless steel Railing System. All drawings

general and supplementary conditions including division one specifications apply to this section.

  - Related Sections

Division 5: Ornamental Handrails and Railings.

1.3	Product References and Design Requirements

1.3.1    Principle items specified in this section are:

a.  Stainless steel and Stainless/wood combination handrails.

b.  Stainless steel and steel guardrails or other ornamental barrier railings.

c.  Stainless steel or tempered glass infill panels.

d.  Stainless steel perforated, woven or welded infill panels.

e.  Stainless steel horizontal or picket infill rods.

f.  Resin infill panels.

g.  Stainless steel rail with LED light insert.

1.3.2	Design requirements are based on IBC/IRC and ADA standards:

a.  Guardrails and handrails shall meet or exceed all applicable building codes.

b.  Railings shall have high strength stainless steel to comply with structural requirements with an appropriate safety margin.

c.  All internal members shall be stainless steel, aluminum or nylon to eliminate the possibility of rust.

d.  Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

1.3.3	Work Included

Provide all materials, labor and equipment necessary to fabricate and completely install 		handrails, guardrails, infill panels, and other railing options as shows on drawings or 			specific herin.

1.3.4	Definitions

Terms and definitions from ASTM E985 and ISO/TC 59 for railing related items apply to 		this section.

1.4	System Performance Requirements

1.4.1	Railings shall meet or exceed the requirements of all applicable building codes.

1.4.2	Railings shall have high strength stainless steel in order to comply with 1.41 with 			adequate safety margin.

1.4.3	All internal members shall be stainless steel, nylon or wood to eliminate the possibility of 		rust.

1.4.4	Prevent galvanic action and other forms of corrosion by insulating metals and other 			materials from direct contact with incompatible materials.

  - Submittals

    - Shop Drawings for architectural approval, showing fabrication and installation of 	handrails and railings including plans, elevations, sections, details of components and 	attachments to other units of work.

    - Product data for stainless steel/wood products to be supplied by the manufacturer.

    - Structural computations or test data/evaluations, material properties, PE (professional 	engineering) calculations signed/sealed in the State of the project, and other information 	needed to ensure satisfactory structural compliance to applicable building codes to be 	supplied by the manufacture, based on final fabrication drawings and documents.

    - Maintenance instructions: Provide manufacturer‘s maintenance and cleaning 	instructions.

    - Warranty: Provide manufacturer‘s warranty effective from completion of work.

    - Initial selection

Provide 6“ long handrail samples complete with supports and rosette covers to 	demonstrate stainless steel grade and finish. Nylon components to be includes if 	specified, color as indicated.

    - Final verification

Qualification data for authorized installers specified in Quality Assurance is to 	demonstrate their capabilities and experience. Include list of completed projects with 	project and architect names.

  - Quality Assurance

    - Single Source Responsibility: Materials shall be supplied by HDI Railing Systems, 3905 	Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

Regionally based Sales Managers available.

    - Execution tolerance plus/minus 5/64” (2 mm).

  - Storage

1.7.1    Store handrails and railing systems in clean, dry location, away from uncured concrete 			and masonry, protected against damage of any kind.

1.7.2	Materials must be kept in original packing until installation.

1.7.3	Materials to be stored at not lower than -40°C (-104°F) or higher than 100°C (212°F).

1.8       Project Conditions

1.8.1	All measurements for handrails and railings should be taken from construction site 			elements to which railings are to fasten. This information to be recorded on final shop 			drawings.

1.8.2	Coordinate fabrication schedule with construction progress to avoid delay of work

Part 2 - Product:

  - Manufacturer

2.1.1.	Mechanically fastened Stainless steel railing systems

Manufacturer shall be HDI Railing Systems, an established U.S. manufacturer of a 			custom pre-engineered, mechanically fastened guardrail and handrail systems, in strict 		compliance with all technical requirements of the drawings and specifications. 				Miscellaneous metal fabricators/suppliers will not be acceptable. This standard is based 		on HDI Railing Systems, 3905 Continental Drive, Columbia PA 17512 (Tel. 				717.285.4088 Fax. 717.285.5083).

2.1.2	Substitutions:  Not permitted.

2.2       Materials for Guardrails and Handrail System

    - All rails and other tubular components shall be constructed using the following:

2.2.1.1   Stainless steel grade AISI, type 304/304L or 316/316L; surface to be 240 			grain/grit finish; tubes 1-1/2” (38mm) outside diameter by 5/64” (2 mm) wall 			thickness.

      - Optional natural wood handrails and top rails are connected to stainless steel 				true bar secured to posts using stainless steel T-connectors on top of posts: 				Standard wood types are available in natural beech, birch or maple, other wood 			types available upon request. All custom stains are subject to customer approval 			and require customer samples. Stainless steel true bar to be inserted into the 				underside of the wood as a structural element; wood is slotted to receive the true 			bar. All bends required for either sloped rail or other necessary changes in 				direction to be manufactured from stainless steel with a 240grit finish to match 				posts and other stainless steel fittings. Transitions from wood to stainless steel 				either at posts or at bends to be smooth and without burrs.

    - All posts and other components shall be constructed using the following:

      - Post steel to be type A36 – 2“ (50mm) by ¼“ (6mm).Hardware attachment 			surface to be on inside of post formed from the post bar. Attaching hardware to 			be fastened by vertically sliding clamps. All steel to be powder coated to required 		color (standard listed 	herein) or custom RAL® color:

49-66230	Light Bronze

49-50024	Forest Green

39-800	20	Cobalt Black

39-60060	Antique Bronze

49-11280	Off White

49-40033	Tanzanite Blue

349-79680	Slate Grey

49-37900	Ruby Red

33-9740	Stardust Silver

    - Surface and side mount fastening plates arnd clamps to be made from steel 			type A36.All steel to be powder coated to required color.

      - Clamps, and block at top of post and handrail attachment all to be Stainless 			Steel grade UNS 1.4305, type 304. Surface to be 240 grain/grit (#6) finish to 			match handrail finish.

      - Salt water and chlorinated swimming pool environments require stainless steel 		grade 	316  or 316L and an Exterior grade Powder Coating formulation; stainless 		steel surface 	to be 240 grain/grit finish; component parts are dimensionally 			equivalent to those described in 2.2.2.

    - Fastening bolts to be stainless steel or other high strength material as 				determined by engineering requirements.

    - Exterior and aggressive environments require stainless steel grade 316 or 			316L to minimize maintenance requirement; surface to be 240 grain/grit (#6) 			finish.

2.3       Glass products, glazing and infill materials

    - Tempered glass:  Provide fully tempered safety glass with polished edges and dubbed (blunt) corners complying with ASTM C1048.  Kind FT (fully tempered), condition A (un-coated).  Types 1 (transparent glass, flat), quality Q3 (glazing select), class, thickness and manufacturing process as indicated below.

2.3.2	Clear glass: Class 1 clear

2.3.3	Tinted glass: Class 2 (tinted heat absorbing and light reducing). Manufacturer’s standard tint color indicated below:

a.	Bronze, Gray, or other as indicated

b.	Low iron

c.	Custom pattern, art glass, etch, edges or surface, laminate or embeds, as specified herein.

    - Allowable thickness 3/8" (9 mm) to 1/2" (13 mm) to be noted on final shop drawings.

2.3.5	Manufacturing process: Manufacture fully tempered glass by horizontal (roller hearth)

process with roll wave distortion parallel with bottom edge of glass as installed.

2.4	Stainless perforated, woven or welded metal infill panels

    - Perforated metal infill panels

Stainless steel perforated metal infill panels with continuous frame by HDI Railing 	Systems. Installed post centers are required complete with sketch, to allow panel 	fabrication. Standard pattern to be 3/8“ square holes on ½“ centers surrounded by a 	continuous 3/8“ x 1.5“ 304 SS rectangular tube frame with hairline joints. Grain is 240 	grit and polished longitudinally to the mitre cuts.

    - Woven or welded metal infill panels

Stainless steel woven or welded infill panels with continuous ½“ x 1.5“ 304 SS 	rectangular tube frame with hairline joints by HDI Railing Systems. Installed post centers 	are required complete with sketch, to allow panel fabrication. Finish is brushed and 	polished. Manufacturers Panel Design indicated below using Stainless steel bars woven 	to create a linked pattern, framed with rectangular SS frame:

        - Stainless steel bars formed into rounded shapes woven to create a linked 		pattern

        - Stainless steel flat bars woven to create a linked pattern

        - Stainless steel bars woven into a rectangular pattern

        - Custom pattern as specified herin

2.5	Stainless steel infill rails

2.5.1		Stainless steel infill rods, max. 9 ea. with guardrail height 42“. Infill rails to be 5/8“ 			O.D. solid stainless steel. Other infill rod O.D. to be indicated. Brushed finish #6 			polished radially. Clamping knobs and fixtures to be stainless steel finished to 				match. Horizontal infill rails on approx. 4“ centers, gaps between rods and 				adjacent posts to be equalized depending on required rail length and site 				conditions (not to exceed 4“) .

2.6	Stainless steel picket rails

2.6.1		Stainless steel solid vertical picket rails 3/8“ (9mm) supported by upper and lower 			rails 5/8“ (15mm * 2mm). Picket rails on approx. 4“ centers, gaps between 				pickets and adjacent posts to be equalized depending on required rail length and 			site conditions (not to exceed 4“). Brushed finish #6 on vertical picket is to be 				lengthwise (vertically oriented), upper and lower supports to be polished radially. 			Clamping knobs and fixtures to be stainless steel finished to match.

2.7   Woven Cable Infill Mesh panels

2.7.1		Material:  Stainless steel, AISI 316L; wire rope diameter 1.5mm

spaced with offset sleeves.

2.7.2 	Horizontal mesh (standard) with offset sleeves positioned horizontally.

2.7.3		Aperture opening 75 – 80mm measured vertically.

2.7.4		Panel frame 5/8” diameter with mitered corners type 304 or type 316

2.7.5		Woven mesh panels attached to posts with standard attachment bar clamp.

2.8	Resin infill panels – blend of polyester resin for interior applications

    - Panel design: flammability results equivalent to Class A for most panel 				configurations; most panels made from 30%-60% recycled content. 				Manufacturers panel design to be indicated below:

    - Material options: indicate textiles, botanicals, prints, textures or Pure colors 			(Pure Colors have  no embed or interlayer; indicate Pantone® color)

    - Color: Indicate clear or specify color(s) to accent/contrast with interlayer; indicate 		Pantone® color(s) for layers

    - Finish: indicate textured (one or both sides); matte or gloss; indicate edge finish

    - Embedded material for three dimensional effect within resin panel:

    - indicate embedded material such as fabric, pine needles, glass fragments

    - indicate color of embedded material

  - LED lighting inserts (LED components subject to change; contact Manufacturer for most 	current LED specifications)

    - Stainless steel rail with LED light strip inserts grade UNS 1.4305, type 304 or 			type 316; surface to be # 6 finish (240 grain/grit); tubes 1.5” (38mm) outside 			diameter by 	.075“ to .090” (1.5 mm – 2.3mm) wall thickness.

    - LED light strip inserts with a beam spread of 45 degrees to 90 degrees, or 			asymmetrical beam spread of 28 degrees and 65 degrees off nadir. Other beam 		spreads available; contact the manufacturer.

    - Standard clear lens; frosted lens optional.

    - Light output at 42“guard height, lumens per ft as indicated, ranging from 36.8 to 			616 lumens per ft dependent on standard or high output and symmetrical or 			asymmetrical.

    - Color temperature as indicated, ranging from 2700K (Kelvin) to 6500K, 				dependent on lumens per ft and beam spread required.

    - Electrical supply for LED strip inserts to be 120-277Volt supply for 24 volt remote 		power 	supply. (Power supply range 20-240watts)

    - Transition sleeves for intermediate supports, backing strips for LED light strips, 			slotted tube inserts and mounting clips by HDI provided as required.

    - Power supply low voltage dimmers available.

2.10	Fasteners

Anchors shall be fabricated from stainless steel or other materials as determined by engineering requirements with capability to sustain, without failure, load imposed within a safety factor of 4, as determined by testing per ASTM E488.

2.11      Fabrication

    - Fabricate railing system for compliance with structural requirements of applicable 		code.

    - Pre-assemble railings prior to shipping to greatest extent possible to minimize 			field splicing and assembly. Disassemble units only as necessary for shipping 			and handling limitations. Clearly mark units for re-assembly and for coordination 		with shop drawings.

2.11.3	Stainless steel tubing cuts shall be square, without burrs and where exposed, 				rounded to produce smooth rigid and hairline joints.

Part 3 – Execution:

3.1       Examination

3.1.1	Do not begin installation until substrates have been properly prepared.

3.1.2	Verify that reinforcement and anchoring devices are the correct type, have been located correctly, and have been installed properly.

3.1.3	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

3.2	Preparation

Provide information on fastening point locations for posts where necessary to relevant parties.

3.3	Installation

Installation shall be by HDI Railing Systems or a qualified, authorized representative of the manufacturer. HDI Railing Systems, 3905 Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

    - Installation must be in accordance with standard or non-standard, yet applicable details

(instructions) included on installation/shop drawings provided by HDI Railing Systems.

3.3.2	Install components plumb and in-line, accurately fitted, free from distortion or defects and securely anchored to structure.

3.3.3	Provide anchors, plates, angles, etc., necessary for connecting railings to structure.

3.3.4 	Any and all field welding shall be by a certified welder.

3.3.5	Access for anchors that require through bolting either vertically or horizontally to be made available through General Contractor.

Erection tolerances

    - Maximum variation from plumb shall be 1/4".

    - Maximum offset from true alignment for every 50-foot of railing shall be 1/4", non-	accumulative.

3.4	Cleaning and Protection

    - Remove manufacturer's protective coverings from exposed surfaces after installation.

    - Railings shall be cleaned, including infill panels, by contractor to the satisfaction of the 	owner.

    - Wipe with moistened cloth only.  Do not use cleaning agents with abrasive or 	acid/alkaline content.

    - General contractor to provide protective covering on handrails and guardrails if 	construction is not yet finished in the area where the railings are installed.

    - Railings shall be cleaned, including infill panels, by contractor to the satisfaction of the 	owner.

    - Wipe with moistened cloth only.  Do not use cleaning agents with abrasive or 	acid/alkaline content.

  - Correction of deficiencies

All deficiencies in work and/or items not meeting specified requirements shall be corrected in

order to meet specification requirements at no additional cost to owner.

End of Section