CSI Format Specification for Circum™ railings – with Infill and LED options

Part 1 - General:

  - Section Includes

Pre-engineered Circum™ Round post stainless steel Railing System. All drawings, general and

supplementary conditions including division one specifications apply to this section.

  - Related Sections

Division 5: Ornamental Handrails and Railings

1.3	Product References and Design Requirements

1.3.1    Principle items specified in this section are:

a.  Stainless steel and Stainless/wood combination handrails.

b.  Stainless steel and steel guardrails or other ornamental barrier railings.

c.  Stainless steel or tempered glass infill panels.

d.  Stainless steel perforated, woven or welded infill panels.

e.  Stainless steel horizontal or picket infill rods.

f.   Resin infill panels.

g.  Stainless steel rail with LED light insert.

1.3.2	Design requirements are based on IBC/IRC and ADA standards:

a  Guardrails and handrails shall meet or exceed all applicable building codes.

b.  Railings shall have high strength stainless steel to comply with structural requirements with an appropriate safety margin.

c  All internal members shall be stainless steel, aluminum or nylon to eliminate the possibility of rust.

d  Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

1.3.3	Work Included

Provide all materials, labor and equipment necessary to fabricate and completely install 		handrails, guardrails, infill panels, and other railing options as shows on drawings or 			specific herin.

1.3.4	Definitions

Terms and definitions from ASTM E985 and ISO/TC 59 for railing related items apply to 		this section.

1.4	System Performance Requirements

1.4.1	Railings shall meet or exceed the requirements of all applicable building codes.

1.4.2	Railings shall have high strength stainless steel in order to comply with 1.41 with 			adequate safety margin.

1.4.3	All internal members shall be stainless steel, nylon or wood to eliminate the possibility of 		rust.

1.4.4	Prevent galvanic action and other forms of corrosion by insulating metals and other 			materials from direct contact with incompatible materials.

  - Submittals

    - Shop Drawings for architectural approval, showing fabrication and installation of 	handrails and railings including plans, elevations, sections, details of components and 	attachments to other units of work.

    - Product data for stainless steel/wood products to be supplied by the manufacturer.

    - Structural computations or test data/evaluations, material properties, PE (professional 	engineering) calculations signed/sealed in the State of the project, and other information 	needed to ensure satisfactory structural compliance to applicable building codes to be 	supplied by the manufacturer, based on final fabrication drawings and documents.

    - Maintenance instructions: Provide manufacturer‘s maintenance and cleaning 	instructions.

    - Warranty: Provide manufacturer‘s warranty effective from completion of work.

    - Initial selection

Provide 6“ long handrail samples complete with supports and rosette covers to 	demonstrate stainless steel grade and finish. Nylon components to be includes if 	specified, color as indicated.

    - Final verification

Qualification data for authorized installers specified in Quality Assurance is to 	demonstrate their capabilities and experience. Include list of completed projects with 	project and architect names.

  - Quality Assurance

    - Single Source Responsibility: Materials shall be supplied by HDI Railing Systems, 	3905 Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

www.hdirailings.com Regionally based Sales Managers available.

    - Execution tolerance plus/minus 5/64” (2 mm).

  - Storage

1.7.1    Store handrails and railing systems in clean, dry location, away from uncured concrete 			and masonry, protected against damage of any kind.

1.7.2	Materials must be kept in original packing until installation.

1.7.3	Materials to be stored at not lower than -40°C (-104°F) or higher than 100°C (212°F).

1.8       Project Conditions

1.8.1	All measurements for handrails and railings should be taken from construction site 			elements to which railings are to fasten. This information to be recorded on final shop 			drawings.

1.8.2	Coordinate fabrication schedule with construction progress to avoid delay of work

Part 2 - Product:

  - Manufacturer

2.1.1.	Mechanically fastened Stainless steel railing systems

Manufacturer shall be HDI Railing Systems, an established U.S. manufacturer of a 			custom pre-engineered, mechanically fastened guardrail and handrail systems, in strict 		compliance with all technical requirements of the drawings and specifications. 				Miscellaneous metal fabricators/suppliers will not be acceptable. This standard is based 		on HDI Railing Systems, 3905 Continental Drive, Columbia PA 17512 (Tel. 				717.285.4088 Fax. 717.285.5083).

2.1.2	Substitutions:  Not permitted.

2.2       Materials for Guardrails and Handrail System

    - All hand rails and other tubular components shall be constructed using the following:

2.2.1.1   Stainless steel grade type AISI 304/304L or 316/316L; surface to be 240 			grain/grit finish; tubes 1-1/2” (38mm) outside diameter by 5/64” (2 mm) wall 			thickness.

      - When using cable as infill rails, all top rail to be Stainless steel grade AISI, type 	304 or 316,  surface to be 240 grain/grit finish; tubes 1-1/2” (38mm) diameter by 	0.145“ (3.7mm) wall thickness.

      - Optional natural wood handrails and top rails to be connected to stainless steel 			true bar secured to posts using stainless steel T-connectors on top of posts: 				Mitered joints required by changes in direction require stainless steel true bar to 			be inserted into the underside of the wood. Standard wood  types are available in 			natural beech, birch or maple, other wood types available upon request. All 				custom stains are subject to customer approval and require customer samples. 				Wood to be continuous throughout. Returns to wall or floor that require 					stainless steel bends should have transitions that are smooth and without burrs.

    - All posts and other components shall be constructed using the following:

2.2.2.1   Stainless steel grade AISI type 304 or 316, surface to be 240 grain/grit finish; 			tubes 1.9” (49mm) diameter by 0.109“ (2.8 mm)wall thickness.

2.2.2.2    Stainless steel grade AISI type 304 or 316, surface to  be 240 grain/grit finish 				for: end caps at top of posts. Hardware for handrail attachment to match finish of 			posts.

      - Stainless steel grade AISI type 304 or 316, surface to be 240 grain/grit (#6) 	finish for  post fastening base plate

    - Fastening bolts to be stainless steel or other high strength material as determined by 	engineering requirements.

    - Infill Panel clamps to be either Pressure Clamps mounted to posts, clamping infill 	panels between centers of posts. Or Panel holders through bolted to the infill panel with 	a “Glass Link” bar, offseting the glass from the center line of the posts. Infill panel 	thickness can be 3/8” (9.5mm) to ½” (12.7mm) or greater as specified. Panel holder 	heights adjustable in accordance with approved drawings (location is factory set). 	Vertical distance between panel holders must be less than or equal to 25-5/8” (600 mm).

    - Exterior and aggressive environments require stainless steel grade AISI 316 or 316L to 	minimize maintenance requirement; surface to be 240 grain/grit (#6) finish.

2.3       Glass products, glazing and infill materials

    - Tempered glass:  Provide fully tempered safety glass with polished edges and dubbed (blunt) corners complying with ASTM C1048.  Kind FT (fully tempered), condition A (un-coated).  Types 1 (transparent glass, flat), quality Q3 (glazing select), class, thickness and manufacturing process as indicated below. Tempered, laminated glass infill panels are required in railings where there is access to areas below the railing (check local codes).

2.3.2	Clear glass: Class 1 clear

2.3.3	Tinted glass: Class 2 (tinted heat absorbing and light reducing). Manufacturer’s standard tint color indicated below:

a.	Bronze, Gray, or other as indicated

b.	Low iron

c.	Custom pattern, art glass, etch, edges or surface, laminate or embeds, as specified herein.

    - Allowable thickness 3/8" (9.5 mm) to 1/2" (12.7 mm) to be noted on final shop drawings.

2.3.5	Manufacturing process: Manufacture fully tempered glass by horizontal (roller hearth)

process with roll wave distortion parallel with bottom edge of glass as installed.

2.4	Stainless perforated, woven or welded metal infill panels

    - Perforated metal infill panels

Stainless steel perforated metal infill panels with continuous frame by HDI Railing 	Systems. Installed post centers are required complete with sketch, to allow panel 	fabrication. Standard pattern to be 3/8“ (9.5 mm) square holes on ½“ (12.7 mm) centers 	surrounded by a continuous 1/2“ (12.7 mm) x 1.5“ (38 mm) 304 SS rectangular tube 	frame with hairline joints. Grain is 240 grit and polished longitudinally to the miter cuts.

    - Woven or welded metal infill panels

Stainless steel woven or welded infill panels with continuous 1/2“ (12.7 mm) x 1.5“ (38 	mm) 304 SS rectangular tube frame with hairline joints by HDI Railing Systems. Installed 	post centers are required complete with sketch, to allow panel fabrication. Finish is 	brushed and polished. Manufacturers Panel Design indicated below using Stainless 	steel bars woven to create a linked pattern, framed with rectangular SS frame:

      - Stainless steel bars formed into rounded shapes woven to create a linked 		pattern

      - Stainless steel flat bars woven to create a linked pattern

      - Stainless steel bars woven into a rectangular pattern

      - Custom pattern as specified herin

2.5	Stainless steel infill rails

2.5.1	Stainless steel infill rods, max. 9 ea.with guardrail height 42“. Infill rails to be 3/8“ (9.5 			mm) diameter solid stainless steel. Brushed finish #6 polished radially. Clamping knobs 		and fixtures to be stainless steel finished to match. Horizontal infill rails on approx. 4“ 			(100 mm) centers, gaps between rods and adjacent posts to be equalized depending on 		required rail length and site conditions not to exceed 4“ (100 mm).

2.6	Stainless steel picket rails

2.6.1	Stainless steel solid vertical picket rails 3/8“ (9.5 mm) supported by upper and lower rails 		5/8“ (15mm * 2mm). Picket rails on approx. 4“ (100 mm) centers, gaps between pickets 		and adjacent posts to be equalized depending on required rail length and site conditions 		not to exceed 4“ (100 mm). Brushed finish #6 on vertical picket, upper and lower 			supports to be polished radially. Clamping knobs and fixtures to be stainless steel 			finished to match.

  - Stainless steel cable rails, cable hardware and woven cable infill mesh

    - Cables

      - Material:  6 x 7 Type 316 stainless steel strand

      - Diameter: 3/16 inch (5 mm) diameter cable with a minimum breaking strength of

13KN (2,923 pounds)

      - Finish: mill

- ** NOTE TO SPECIFIER ** Select orientation.  Delete three of the following four paragraphs.

      - Orientation:  As indicated on the Contract Drawings

- ** NOTE TO SPECIFIER **  Select spacing requirement.  Delete one of the next two paragraphs.

2.7.1.5     Spacing:  As indicated on the Contract Drawings (max. 3-1/8” - 79mm)

2.7.2   Cable Hardware Components

2.7.2.1    Material:  Stainless steel, AISI 316L; Swaged hardware at end of cable

2.7.2.2    Hardware concealed inside end posts where practical

2.7.2.3    To comply with HDI Railing Systems’ design criteria

2.7.2.4    Types of Fittings: Radius head internal thread adjuster; External thread

swaged end

2.7.3   Woven Cable Infill Mesh panels

2.7.3.1    Material:  Stainless steel, AISI 316L; wire rope diameter 1.5mm

spaced with offset sleeves.

2.7.3.2    Horizontal mesh (standard) with offset sleeves positioned horizontally.

2.7.3.3    Aperture opening 75 – 80mm measured vertically.

2.7.3.4    Panel frame 5/8” (16mm) diameter with mitered corners type 304 or type 			316

2.7.3.5    Woven mesh panels attached to posts with standard attachments.

  - Resin infill panels – blend of polyester resin for interior applications

2.8.1     Panel design: flamability results equivalent to Class A for most panel configurations;

most panels made from 30%-60% recycled content. Manufacturers panel design to be

indicated below:

2.8.1.1   Material options: indicate textiles, botanicals, prints, textures or Pure

colors (Pure Colors have  no embed or interlayer; indicate Pantone®

color)

      - Color: Indicate clear or specify color(s) to accent/contrast with interlayer;

indicate Pantone® color(s) for layers

      - Finish: indicate textured (one or both sides); matte or gloss; indicate

edge finish

2.8.1.4   Embedded material for three dimensional effect within resin panel:

- indicate embedded material such as fabric, pine needles, glass fragments

- indicate color of embedded material

  - LED lighting inserts (LED components subject to change; contact Manufacturer for most current LED specifications)

    - Stainless steel rail with LED light strip inserts grade AISI type 304 or type 316; surface to be # 6 finish (240 grain/grit); tubes 1.5” (38mm) outside diameter by .075“ to .090” (1.5 mm – 2.3mm) wall thickness.

    - LED light strip inserts with a beam spread of 45 degrees to 90 degrees, or asymmetrical beam spread of 28 degrees and 65 degrees off nadir. Other beam spreads available; please contact the manufacturer.

    - Standard clear lens; frosted lens optional.

    - Light output at 42“guard height, lumens per ft as indicated, ranging from 36.8 to 616 lumens per ft dependent on standard or high output and symmetrical or asymmetrical.

    - Color temperature as indicated, ranging from 2700K (Kelvin) to 6500K, dependent on lumens per ft and beam spread required.

    - Electrical supply for LED strip inserts to be 120-277Volt supply for 12 or 24 volt remote power supply. (Power supply range 20-240watts)

    - Transition sleeves for intermediate supports, backing strips for LED light strips, slotted tube inserts and mounting clips by HDI provided as required.

    - Power supply low voltage dimmers available.

2.10	Fasteners

Anchors shall be fabricated from stainless steel or other materials as determined by engineering requirements with capability to sustain, without failure, load imposed within a safety factor of 4, as determined by testing per ASTM E488.

2.11    	  Fabrication

2.11.1   Fabricate railing system for compliance with structural requirements of applicable code.

2.11.2  Pre-assemble railings prior to shipping to greatest extent possible to minimize field 			splicing and assembly.  Disassemble units only as necessary for shipping and handling 		limitations.  Clearly mark units for re-assembly and for coordination with shop drawings.

2.11.3  Stainless steel tubing cuts shall be square, without burrs and where exposed, rounded 			to produce smooth rigid and hairline joints.

Part 3 – Execution:

3.1       Examination

3.1.1	Do not begin installation until substrates have been properly prepared.

3.1.2	Verify that reinforcement and anchoring devices are the correct type, have been located correctly, and have been installed properly.

3.1.3	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

3.2	Preparation

Provide information on fastening point locations for posts where necessary to relevant parties.

3.3	Installation

Installation shall be by HDI Railing Systems or a qualified, authorized representative of the manufacturer. HDI Railing Systems, 3905 Continental Drive, Columbia PA 17512 (Tel: 717-285-4088 Fax 717-285-5083).

    - Installation must be in accordance with standard or non-standard, yet applicable details

(instructions) included on installation/shop drawings provided by HDI Railing Systems.

3.3.2	Install components plumb and in-line, accurately fitted, free from distortion or defects and securely anchored to structure.

3.3.3	Provide anchors, plates, angles, etc., necessary for connecting railings to structure.

3.3.4 	Any and all field welding shall be by a certified welder.

3.3.5	Access for anchors that require through bolting either vertically or horizontally to be made available through General Contractor.

Erection tolerances

    - Maximum variation from plumb shall be 1/4" (6mm).

    - Maximum offset from true alignment for every 50-foot of railing shall be 1/4" (6 mm), 	non-accumulative.

3.4	Cleaning and Protection

    - Remove manufacturer's protective coverings from exposed surfaces after installation.

    - Railings shall be cleaned, including infill panels, by contractor to the satisfaction of the owner.

    - Wipe with moistened cloth only.  Do not use cleaning agents with abrasive or acid/alkaline content.

    - General contractor to provide protective covering on handrails and guardrails if construction is

not yet finished in the area where the railings are installed.

    - Railings shall be cleaned, including infill panels, by contractor to the satisfaction of the owner.

    - Wipe with moistened cloth only.  Do not use cleaning agents with abrasive or acid/alkaline content.

  - Correction of deficiencies

All deficiencies in work and/or items not meeting specified requirements shall be corrected in

order to meet specification requirements at no additional cost to owner.

End of Section